To measure and compare Raman spectra of Rhodamine 6G (R6G) at concentrations of 10⁻² M, 10⁻³ M, and 10⁻⁴ M using chromatography paper and two Raman systems: a lab desk laser system and a portable Raman device. Then, evaluate spectral change by sliding the samples under the portable Raman head.

Materials

- R6G solution

- Deionized (DI) water

- Pipettes and tips

- Chromatography paper strips

- Silicone sheet (flat and clean)

- Benchtop Raman microscope (785 nm laser)

- Portable Raman spectrometer

- Petri dishes

- Gloves and tweezers

- Labels or markers

Part 1: Sample Preparation

1.  Dilution:

- Prepare 3 dilutions of R6G:

- 10⁻² M

- 10⁻³ M

- 10⁻⁴ M

- Use DI water for all dilutions and store in labeled containers.

2.  Paper preparation:

- Cut chromatography paper into 4 strips per concentration (One for just the paper).

- Label each strip (e.g., “10⁻²”, “10⁻³”, “10⁻⁴”).

3.  Soaking:

- Pipette 50 µL of each R6G dilution onto a strip.

- Allow to dry completely (~10 min in air).

Part 2: Raman Measurement – Lab Desk Laser

4.  Mount one strip of each concentration on a flat, non-reflective surface (ex. silicon slide).

5.  Use appropriate objectives (ex. 10× or 20×).

6.  Focus on the paper/dyed region on the strip.

7.  Set accumulation/WITec parameters (ex. integration time, num of points).

8.  Record spectra for each concentration.

9.  Export spectra

Part 3: Raman Measurement – Portable Raman

10.  Mount new strips of each concentration on a stable platform (ex. silicone slide).

11.  Use portable Raman to scan each sample individually.

12.  Make sure the laser is in focus.

13.  Record Raman spectra for each.

14.  Label and export data

Part 4: Sliding Sample Protocol

15.  Align the remaining set of 3 paper strips (one per concentration) on a silicon sheet:

- Arrange them in a row with minimal spacing.

- Use a small strip of tape to keep them flat and in place.

16.  Place the silicon sheet on a platform where it can be gently slid.

17.  Start with the lowest concentration (or plain paper) under the portable Raman laser.

18.  Take the spectrum.

19.  Slide gently so that the next sample moves into the laser spot.

20.  Repeat for all three concentrations, keeping exposure time and settings constant.

21.  Export data and note approximate positions or transition points.